# AOS   AO3403  Reliability Test Report

PACKAGE TYPE：SOT-23

| Approval | Prepared By | Date |
| --- | --- | --- |
| Wilson Ma | QA Dept. | Sept 27, 2002 |

The qualification of all AOS parts consist of two qualifying processes:

- The Package or Assembly Family Qualification

- The Silicon Technology Qualification

Tests were performed in accordance with our spec requirement and applicable

Mil-Std-883 or JEDEC specifications.

The package will be subjected to the following tests :

Qualification Test Name			Qualification Test Method

Pre-Conditioning				JEDEC JESD22-A113

HAST						JEDEC JA101-A110

Temperature Cycling ( T/C )			JEDEC JA104, MIL-STD-883

Pressure Pot ( P/P )				JEDEC JA102

Bond Integrity					JEDEC JB116, M2011

Solderability					MIL-STD-883 M2003

Die Shear					MIL-STD-883 M2019

DPA						AOS Requirement

C-SAM					AOS Requirement

For Silicon Technology Qualification, the devices will be subjected to two major tests :

High Temperature Gate Bias ( HTGB )

The HTGB test biases gate or other oxides of the device samples. The devices are normally operated in a static mode at, or near, maximum-rated oxide breakdown voltage levels. The particular bias conditions should be determined to bias the maximum number of gates in the device. . In AOS MOSFETs, we apply 100% of rated VGS,MAX at 150C between the gate and source, with Vds=0V.

High Temperature Reverse Bias ( HTRB )

The HTRB test is configured to reverse bias major power handling junctions of the device samples. The devices are characteristically operated in a static operating mode at, or near, maximum-rated breakdown voltage and/or current levels. The particular bias conditions should be determined to bias the maximum number of the solid state junctions in the device. In AOS MOSFETs, we apply 80% of rated VDS,MAX at 150C to the Drain-Source junction, with Vgs=0V.

The AOS part will be considered qualified only after both qualifications tests have been passed.

1. Result of the package qualification tests are summarized as follows :

2. The Silicon Technology Qualification test data is summarized as follows :

HTGB SUMMARY:

1st  Lot :

2nd Lot

3rd Lot

HTRB SUMMARY:

1st Lot

2nd Lot

3rd Lot